CC.Fast Yellow HPX07

- PRODUCT:

Name			:  CC.Fast Yellow HPX07

Chemical Class		:  Diarylide

Colour Index Name	:  Pigment Yellow 83

Colour Index No.		:  21118

CAS No.		:  5567-15-7

EINECS No.		: 226-939-8

Substance Name		: 2,2'-[(3,3'-dichloro[1,1'-biphenyl]-4,4'-diyl)bis(azo)]bis[N-(4-chloro-2,5-dimethoxyphenyl)-3-oxobutyramide]

Molecular Formula	: C36H32Cl4N6O8

- PHYSICAL PROPERTIES:

Density		:   1,45 - 1,55 gr / cm³		Specific Surface		: 65 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  40 - 45 ml / 100 g

pH 		:  6 to 8

Heat stability       :  200 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 200 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 - 6				Tint Tone (1:10)		   : 5 - 6

- WEATHER FASTNESS  :

6 Months	:  5 				12 Months		   : 5 - 4

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Ethanol		: 4 - 5		Ethyl Acetate	: 4		MEK	: 3 - 4

Butanol		: 4 - 5		Butyl Acetate	: 3 - 4		DOP	: 4 - 5

Toluene		: 4 		White Spirit 	: 5		DBP	: 4 - 5

Paraffin Wax	: 5		Butter		: 5		Soap	:5

Water		: 5		Linseed Oil	: 5		Cellosolve:

- TECHNICAL COMMENTS:

CC.Fast Yellow HPX07  is a very strong, red shade, highly opaque diarylide yellow pigment. It exhibits excellent light fastness properties as well as good overall fastness properties. High opacity for an organic pigment. As it has very good flow properties in paints, it can also be used at high pigment concentrations (about 20 % pigment relative to solid binder) without affecting the gloss.

7.  APPLICATIONS:

Suitable for the production of intense opaque yellow shades for lead-free or low-lead paints in all systems.