CC.Perf Blue A3R

- PRODUCT:

Name			:  CC.Perf Blue A3R

Chemical Class		:  Indanthrone

Colour Index Name	:  Pigment Blue 60

Colour Index No.		:  69800

CAS No.		:  81-77-6

EINECS No.		:  201-375-5

Substance Name		:  6,15-dihydroanthrazine-5,9,14,18-tetrone

Molecular Formula	: C28H14N2O4

- PHYSICAL PROPERTIES:

Density		:   1,60 – 1,65 gr / cm³		Specific Surface		: 57 m² / gr

Moisture Content  : Max. 0.5%			Water Soluble Content	: Max. 0.5%

Oil Absorption     :  30 - 35 ml / 100 g

pH 		:  6 to 8

Heat stability       :  300 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 300 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  8				Tint Tone (1:10)		   : 8

- WEATHER FASTNESS  :

6 Months	:  5				12 Months		   : 5

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 5		MEK	: 5

Butanol		: 5 		Butyl Acetate	: 5		DOP	: 5

Toluene		: 5 		White Spirit 	: 5  		DBP	: 5

Paraffin Wax	: 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 5		Cellosolve: 5

- TECHNICAL COMMENTS:

CC.Perf Blue A3R is a very red shade Indanthrone Blue pigment having very high fastness properties. The product has excellent weather and light fastness. Indanthrone Blue 60 has much better weather, heat and light fastness properties compared to Phthalocyanine pigments.

- APPLICATIONS:

Product is suggested for plastics and fiber applications.