CC.Perf Ecarlate R

- PRODUCT:

Name			:  CC.Perf Ecarlate R

Chemical Class		:  Perylene

Colour Index Name	:  Pigment Red 123

Colour Index No.		:  71145

CAS No.		:  24108-89-2

EINECS No.		: 246-018-4

Substance Name		: 2,9-bis(4-ethoxyphenyl)anthra[2,1,9-def:6,5,10-d'e'f']diisoquinoline-1,3,8,10(2H,9H)-tetrone

Molecular Formula	: C40H26N2O6

- PHYSICAL PROPERTIES:

Density		:   1,45 – 1,50 gr / cm³		Specific Surface		: 80 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  65 ml / 100 g

pH 		:  6 to 8

Heat stability       :  300 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 300 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  8				Tint Tone (1:10)		   : 7 - 8

- WEATHER FASTNESS  :

6 Months	:  5 - 6				12 Months		   : 5

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 5		MEK	: 5

Butanol		: 5 		Butyl Acetate	: 5		DOP	: 5

Toluene		: 5 		White Spirit 	: 5  		DBP	: 5

Paraffin Wax	: 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 5		Cellosolve: 5

- TECHNICAL COMMENTS:

Pigment Red 123 is a yellow shade perilene pigment with the outstanding fastness properties of this group of pigments. It is yellower than Pigment Red 122.

With high tintorial strength and out-standing fastness to light and weathering at a very wide range of concentrations. Is used in combination with opaque organic orange pigments or molybdate orange for very pure reds and in metallic paints for purple shades and as a shading pigment.

Suitable for high-tech applications and for most plastics. Excellent fastness to weathering.

- APPLICATIONS:

Recommended for all types of inks, paints and plastics. Universal.