CC.Perf Carmine HF3C

- PRODUCT:

Name			:  CC.Perf Carmine HF3C

Chemical Class		:  Benzimidazolone

Colour Index Name	:  Pigment Red 176

Colour Index No.		:  12515

CAS No.		:  12225-06-8

EINECS No.		: 235-425-2

Substance Name		: N-(2,3-dihydro-2-oxo-1H-benzimidazol-5-yl)-3-hydroxy-4-[[2-methoxy-5-[(phenylamino)carbonyl]phenyl]azo]naphthalene-2-carboxamide

Molecular Formula	: C32H24N6O5

- PHYSICAL PROPERTIES:

Density		:   1,40 – 1,45 gr / cm³		Specific Surface		: 56 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  45 ml / 100 g

pH 		:  6 to 8

Heat stability       :  270 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 270 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 				Tint Tone (1:10)		   : 7

- WEATHER FASTNESS  :

6 Months	:  4 - 5				12 Months		   : 4 - 5

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Ethanol		: 4		Ethyl Acetate	: 4		MEK	: 4

Butanol		: 4 		Butyl Acetate	: 5		DOP	: 4 - 5

Toluene		: 4 - 5 		White Spirit 	: 5  		DBP	: 4 - 5

Paraffin Wax	: 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 5		Cellosolve: 5

- TECHNICAL COMMENTS:

Pigment Red 176  is a blue shade benzimidazolone pigment with the outstanding fastness properties of this group of pigments.

With high tintorial strength and out-standing fastness to light and weathering at a very wide range of concentrations. Suitable for high-tech applications and for most plastics. Excellent fastness to weathering. Excellent dielectric properties.

- APPLICATIONS:

Recommended for paste inks and for solvent- and water based packaging gravure and flexographic printing inks.

Suitable for cable sheathing and spin-dyeing applications.