CC.Perf Bordeaux A3B

- PRODUCT:

Name			:  CC.Perf  Bordeaux A3B

Chemical Class		:  Anthraquinone

Colour Index Name	:  Pigment Red 177

Colour Index No.		:  65300

CAS No.		:  4051-63-2

EINECS No.		: 223-754-4

Substance Name		: 4,4'-diamino[1,1'-bianthracene]-9,9',10,10'-tetraone

Molecular Formula	: C28H16N2O4

- PHYSICAL PROPERTIES:

Density		:   1,50 – 1,55 gr / cm³		Specific Surface		: 44 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  65 ml / 100 g

pH 		:  6 to 8

Heat stability       :  290 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 290 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 - 8				Tint Tone (1:10)		   : 7

- WEATHER FASTNESS  :

6 Months	:  4 - 5				12 Months		   : 4 - 5

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Ethanol		: 4 - 5		Ethyl Acetate	: 4 - 5		MEK	: 4 - 5

Butanol		: 4 - 5 		Butyl Acetate	: 4 - 5		DOP	: 4 - 5

Toluene		: 4 - 5 		White Spirit 	: 4 - 5  		DBP	: 4 - 5

Paraffin Wax	: 5		Butter		: 4 - 5		Soap	: 5

Water		: 5		Linseed Oil	: 4 - 5		Cellosolve: 5

- TECHNICAL COMMENTS:

Pigment Red 177  is a very dark blue shade anthraquinone pigment with the outstanding fastness properties of this group of pigments.

With high tintorial strength and out-standing fastness to light and weathering at a very wide range of concentrations. Is used in combination with opaque organic orange pigments or molybdate orange for very pure reds and in metallic paints for purple shades and as a shading pigment.

Suitable for high-tech applications and for most plastics. Excellent fastness to weathering.

- APPLICATIONS:

High quality industrial coating finishes, foil coating lacquers and metallic finishes.

Printing Inks, plastics and rubber.