CC.Perf Scarlet Pink EG

- PRODUCT:

Name			:  CC.Perf Scarlet Pink EG

Chemical Class		:  Quinacridone

Colour Index Name	:  Pigment Red 209

Colour Index No.		:  73905

CAS No.		:  3089-17-6

EINECS No.		:  221-424-4

Substance Name		:  1,8 Chloro Quinacridone

Molecular Formula	: C20H10O2N2Cl2

- PHYSICAL PROPERTIES:

Density		:   1,60 – 1,65 gr / cm³		Specific Surface		: 42 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  54 ml / 100 g

pH 		:  6 to 8

Heat stability       :  290 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 280 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 - 8 				Tint Tone (1:10)		   : 7 - 8

- WEATHER FASTNESS  :

6 Months	:  4 - 5				12 Months		   : 4 - 5

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 5		MEK	: 5

Butanol		: 5 		Butyl Acetate	: 5		DOP	: 5

Toluene		: 5 		White Spirit 	: 5  		DBP	: 5

Paraffin Wax	: 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 5		Cellosolve: 5

- TECHNICAL COMMENTS:

Pigment Red 209  is highly transparent and the most yellowish red shade quinacridone pigment with the outstanding fastness properties of this group of pigments.

- APPLICATIONS:

Highly recommended for high performance coatings and automotive paints.

Recommended for paste inks and for solvent- and water based packaging gravure and flexographic printing inks.

Recommended for PVC and suitable for polyolefins.