CC.Perf Red DPP C

- PRODUCT:

Name			:  CC.Perf Red DPP C

Chemical Class		:  Diketopyrrolopyrrole

Colour Index Name	:  Pigment Red 255

Colour Index No.		:  561050

CAS No.		:  54660-00-3

EINECS No.		:

Substance Name		: Bis-(p-pheny)-1.4-diketopyrrolo(3.4-c)pyrrole

Molecular Formula	: C18H12N2O2

- PHYSICAL PROPERTIES:

Density		:   1,40 – 1,45 gr / cm³		Specific Surface		: 10.5 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  58 ml / 100 g

pH 		:  7 to 8

Heat stability       :  350 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 350 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  8				Tint Tone (1:10)		   : 8

- WEATHER FASTNESS  :

6 Months	:  4 - 5				12 Months		   : 4 - 5

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Ethanol		: 4		Ethyl Acetate	: 4  		MEK	: 3 - 4

Butanol		: 4  		Butyl Acetate	: 4 		DOP	: 4

Toluene		: 5  		White Spirit 	: 5  		DBP	: 3 - 4

Paraffin Wax	: 5		Butter		: 4 		Soap	: 5

Water		: 5		Linseed Oil	: 4 - 5		Cellosolve: 5

- TECHNICAL COMMENTS:

CC.Perf Red DPP C is a brilliant high-performance yellowish mid-shade red with excellent dispersibility, high color strength, high opacity and outstanding fastness and resistance properties.

- APPLICATIONS:

High quality industrial coating finishes, foil coating lacquers and metallic finishes.

Printing Inks (liquid and offset), silk screen inks, inks for laminated paper and plasticizer based, PVC.