CC.Perf Yellow 3RLP

- PRODUCT:

Name			:  CC.Perf  Yellow 3RLP

Chemical Class		:  Isoindolinone Pigment

Colour Index Name	:  Pigment Yellow 110

Colour Index No.		:  56280

CAS No.		:  5590-18-1

EINECS No.		:  226-999-5

Substance Name		:  3,3'-(1,4-phenylenediimino)bis[4,5,6,7-tetrachloro-1H-isoindol-1-one]

Molecular Formula	: C22H6N4O2Cl8

- PHYSICAL PROPERTIES:

Density		:   1,8 - 1,85 gr / cm³		Specific Surface		: 28 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  38 ml / 100 g

pH 		:  3.5 to 7

Heat stability       :  300 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 300 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 - 8				Tint Tone (1:10)		   : 7 - 8

- WEATHER FASTNESS  :

6 Months	:  7 - 6				12 Months		   : 7 - 6

5.   HEAT RESISTANCE :     (°C) Approx

|  | PS | ABS | HDPE | PP |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Transparent : | 260 | 280 | 300 | 300 |  |  |
| Opaque : | 260 | 260 | 300 | 300 |  |  |

6.   FASTNESS PROPERTIES:

Migration             : 4 – 5 (p-PVC)

Ethanol		: 4 - 5		Ethyl Acetate	: 4		MEK	: 3

Butanol		: 4 - 5		Butyl Acetate	: 3 - 4		DOP	: 4

Toluene		: 4 - 5		White Spirit 	: 5		DBP	: 3

Paraffin Wax	: 5		Butter		: 5		Soap	:5

Water		: 5		Linseed Oil	: 5		Cellosolve: 4

7.   TECHNICAL COMMENTS:

Pigment Yellow 110  is a reddish yellow pigment with high transparency. Excellent heat and outstanding fastness properties, especially weathering, even at low concentrations. FDA and FPL listed. Excellent dispersibility in PVC and recommended for all high performance applications.

8.   APPLICATIONS:

Recommended for  Paint, Automotive Paints, Powder paints, all plastics.