CC.Perf Yellow 6GHD

- PRODUCT:

Name			:  CC.Perf  Yellow 6GHD

Chemical Class		:  Quinophthalone Pigment

Colour Index Name	:  Pigment Yellow 138

Colour Index No.		:  56300

CAS No.		:  30125-47-4

EINECS No.		:  250-063-5

Substance Name		:  3,4,5,6-tetrachloro-N-[2-(4,5,6,7-tetrachloro-2,3-dihydro-1,3-dioxo-1H-inden-2-yl)-8-quinolyl]phthalimide

Molecular Formula	: C26H6N2O4Cl8

- PHYSICAL PROPERTIES:

Density		:   1,8 - 1,85 gr / cm³		Specific Surface		: 28 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  45 ml / 100 g

pH 		:  3.5 to 7

Heat stability       :  290 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 280 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 - 8				Tint Tone (1:10)		   : 7 - 8

- WEATHER FASTNESS  :

6 Months	:  7 - 6				12 Months		   : 7 - 6

- FASTNESS PROPERTIES:

Migration             : 4 - 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 5		MEK	: 4

Butanol		: 5		Butyl Acetate	: 5		DOP	: 4 - 5

Toluene		: 5		White Spirit 	: 5		DBP	: 4 - 5

Paraffin Wax	: 5		Butter		: 5		Soap	:5

Water		: 5		Linseed Oil	: 5		Cellosolve: 4

- TECHNICAL COMMENTS:

Pigment Yellow 138  is a green shade opaque yellow pigment.  Very good chemical and weathering fastness.

- APPLICATIONS:

Recommended for  Paint, Automotive Paints, Powder paints.

Suitable for Plastics polyolefines.