CC.Perf Yellow F2G

- PRODUCT:

Name			:  CC.Perf Yellow F2G

Chemical Class		:  Benzimidazolone

Colour Index Name	:  Pigment Yellow 194

Colour Index No.		:  11785

CAS No.		:  82199-12-0

EINECS No.		: 279-914-9

Substance Name		: N-(2,3-dihydro-2-oxo-1H-benzimidazol-5-yl)-2-[(2-methoxyphenyl)azo]-3-oxobutyramide

Molecular Formula	: C18H17N5O4

- PHYSICAL PROPERTIES:

Density		:   1,45 - 1,50 gr / cm³		Specific Surface		: 20 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  95 ml / 100 g

pH 		:  6 to 8

Heat stability       :  200 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 190 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 - 8				Tint Tone (1:10)		   : 7

- WEATHER FASTNESS  :

6 Months	:  4 - 5				12 Months		   : 4

- FASTNESS PROPERTIES:

Migration             : 4 - 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 3 - 4		MEK	: 3

Butanol		: 4		Butyl Acetate	: 3 - 4		DOP	: 5

Toluene		: 3		White Spirit 	: 4 - 5		DBP	: 4

Paraffin Wax	: 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 5		Cellosolve: 4

- TECHNICAL COMMENTS:

strong, green shade benzimidazolone pigment. It exhibits excellent overall fastness properties as well as good rheological properties.

Greenish high-strength yellow pigment with good rheo-logical properties. Especially suited for economical shade matching in the yellow, orange and green ranges in the industrial paints sector.

- APPLICATIONS:

Recommended for paste inks and for solvent- and water based packaging gravure and flexographic printing inks and industrial paints.