CC.Iroxi Black 722 M

- PRODUCT:

Name			:  CC.Iroxi  Black 722M

Chemical Class		:  Synthetic Iron Oxide

Colour Index Name	:  Pigment Black 11

Colour Index No.		:  77499

CAS No.		:  1317-61-9

EINECS No.		:  215-277-5

Substance Name		:  Tétraoxyde de trifer

Molecular Formula	:  Fe3O4

- PHYSICAL PROPERTIES:

Density		:   4,6 gr / cm³			Specific Surface		: 19 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 0,2%

Oil Absorption     :  15 - 25 ml / 100 g

pH 		:  5 to 7

Heat stability       :  180 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 180 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

Residues (25 µm)	:  0,2 %

- LIGHT FASTNESS  :

Full Tone (1:1)	:  8				Tint Tone (1:10)		   : 8

- WEATHER FASTNESS  :

6 Months	:  5				12 Months		   : 5

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Solvents		: 5

Water		: 5

- TECHNICAL COMMENTS:

Insoluble in water and organic solvents. Completely inert in organic and inorganic binders (cement, ceramic compounds, etc.). Excellent light and weather fastness. Good alkali resistance. Excellent hiding strength.

- APPLICATIONS:

Recommended for cements, papers, paints, ceramics, plastics, rubbers, flooring, etc.