CC.Lake Pink 8110

- PRODUCT:

Name			:  CC.Lake Pink 8110

Chemical Class		:  Basic Red 1 toner, Triaryl carbonium toner

Colour Index Name	:  Pigment Red 81:1

Colour Index No.		:  45160:1

CAS No.		:  80083-40-5

EINECS No.		:  279-394-3

Substance Name		: Xanthylium, 9-[2-(ethoxycarbonyl)phenyl]-3,6-bis(ethylamino)-2,7-dimethyl-, molybdatetungstatesilicate

- PHYSICAL PROPERTIES:

Density		:   1,90 – 2,00 gr / cm³		Specific Surface		: 50 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  70 ml / 100 g

pH 		:  4,5 to 7,0

Acid Resistance	: 5				Alkali Resistance		: 4

- LIGHT FASTNESS  :

Full Tone (1:1)	:  2 - 3				Tint Tone (1:10)		   : 1 - 2

- WEATHER FASTNESS  :

6 Months	:  1				12 Months		   : 1

- FASTNESS PROPERTIES:

Migration             : 4 (p-PVC)

Ethanol		: 2		Ethyl Acetate	: 4 		MEK	: 2

Butanol		: 2 		Butyl Acetate	: 4		DOP	: 5

Toluene		: 5 		White Spirit 	: 5  		DBP	: 5

Paraffin Wax	: 2		Butter		: 1		Soap	: 2

Water		: 4		Linseed Oil	: 5		Cellosolve: 5

- TECHNICAL COMMENTS:

CC.Lake Pink 8110 is a strong and brilliant yellow shade red pigment only suitable for solvent based flexographic inks and paste inks.

- APPLICATIONS:

Recommended for polyamide and Nitrocellulose Inks. Oil inks.