CC.Perf Yellow H4G

- PRODUCT:

Name			:  CC.Perf Yellow H4G

Chemical Class		:  pyrimidinetrione complexe

Colour Index Name	:  Pigment Yellow 150

Colour Index No.		:  12764

CAS No.		:  68511-62-6

EINECS No.		: 270-944-8

Substance Name		: Nickel, 5,5'-azobis-2,4,6(1H,3H,5H)-pyrimidinetrione complexes

Molecular Formula	: C8H6N6O6

- PHYSICAL PROPERTIES:

Density		:   1,5 - 1,6 gr / cm³		Specific Surface		: 23 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  45 - 50 ml / 100 g

pH 		:  6.5 to 7.5

Heat stability (in paint or PVC):  180 C° / 5 min. (Full Tone)             Tint Tone (1:10) : 180 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 3

- LIGHT FASTNESS  :

Full Tone (1:1)	:  8				Tint Tone (1:10)		   : 7 - 8

- WEATHER FASTNESS  :

6 Months	:  5				12 Months		   : 4 - 5

- FASTNESS PROPERTIES:

Migration             : 4 - 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 4 - 5		MEK	: 4 - 5

Butanol		: 4 		Butyl Acetate	: 4		DOP	: 4 - 5

Toluene		: 3 		White Spirit 	: 4 - 5		DBP	: 4 - 5

Paraffin Wax	: 5		Butter		: 5		Soap	:4 - 5

Water		: 5		Linseed Oil	: 4 - 5		Cellosolve:

- TECHNICAL COMMENTS:

Very greenish yellow pigment with excellent fastness to light and weathering, especially in deep shades. Relatively good opacity for an organic pigment. As it has very good flow properties in paints, it can also be used at high pigment concentrations (25 - 30 % pigment relative to solid binder) without affecting the gloss. It should be borne in mind that the resistance to very strong alkalis is unsatisfactory. This pigment is also recommended for plastic application with excellent light fastness, good resistance to migration and excellent thermal stability.

Heat Resistance :     (°C) Approx

|  | PS | HDPE / PP | SAN | PA 6 | PC | PETP |
| --- | --- | --- | --- | --- | --- | --- |
| Full Shade: | 300 | 300 | 300 | 280 | >310 | 300 |
| Tint Shade: | 300 | 300 | 300 | 270 | >310 | 300 |

Additional Technical Properties :

| PET | recommended |
| --- | --- |
| PA 6.6 | limited suitable |
| PA Fiber Applications | Not recommended |