CC.Perf Carbon Black 249G

- PRODUCT:

Name			:  CC.Perf Carbon Black 2429G

Chemical Class		:  Carbon Black

Colour Index Name	:  Pigment Black 7

Colour Index No.		:  77266

CAS No.		:  1333-86-4

EINECS No.		:  215-609-9

Substance Name		:  Carbon Black

Molecular Formula	:  C

- PHYSICAL PROPERTIES:

Density		:   0,36 gr / cm³			Specific Surface		: 82 m² / gr

Moisture Content  : Max. 0,2%			Water Soluble Content	: Insoluble

Oil Absorption     :  102 ml / 100 g

pH 		:  5 to 7

Heat stability       :  3600 C°

Acid Resistance	: 5				Alkali Resistance		: 5

Ash Content	: 0,7

Particle Size (nm) :  5 - 500

- LIGHT FASTNESS  :

Full Tone (1:1)	:  8				Tint Tone (1:10)		   : 8

- WEATHER FASTNESS  :

6 Months	:  5				12 Months		   : 5

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Solvents		: 5

Water		: 5

- TECHNICAL COMMENTS:

Easy dispersion for pipe and film compound

Good dyeing of synthetic fiber

Stable tinting of coating

Good jetness for papers

Good dispersion for carbon paper, newspaper ink, etc.

Also applicable to PU & PVC sealants

- APPLICATIONS:

Main application is plastics, fibers, coatings and inks.