CC.Phos Green 2050

1. Product

Name					:  CC.Phos Green 2050

Class					:  photo-luminescent pigment

Product group              :  Inorganic photo-luminescent pigments for visible effects

Main use                  :  After-glowing plastic sheets, silk screen printing ink, paints,

textile pastes, etc.

2. Typical chemical properties

Composition          :  Alkaline earth aluminate silicate

Molecular Formula		 :  MO.Al2O3SiO2:Eu

Insoluble in           :  organic solvents

Decomposition by      :  Acids, , water, alkalies

3. Typical physical properties

Appearance            :  light yellow

Specific gravity         :  3.6g/cm3

Temperature resistance   :  250 C°

4. Typical luminescent properties

Excitation              :  UV radiation, white light (any visible light)

Excitation wavelength     :  200-450nm

Peak value              :  520nm

Glowing Color           :  yellow-green

Brightness of afterglow    :  >12 hours

According to DIN67510,Part1

5. Brightness testing report

| Item | CC.Phos Green 2050 |
| --- | --- |
| Time(minute) | Brightness (mcd/m2) |
| 0 | 13100 |
| 1 | 2150 |
| 5 | 560 |
| 10 | 292 |
| 20 | 143 |
| 30 | 92 |
| 40 | 66 |
| 50 | 51 |
| 60 | 41 |
| Standard at 10 min | 41 |
| Average Particle Size(um) | 20-50 |

NOTE:

Brightness of the pigment of different production batch will be little different, but we guarantee the product accords with our quality standard.