CC.Phos Green 2535

1. Product

Name					:  CC.Phos Green 2535

Class					:  photo-luminescent pigment

Product group              :  Inorganic photo-luminescent pigments for visible effects

Main use                  :  After-glowing plastic sheets, silk screen printing ink, paints,

textile pastes, etc.

REACH PRE REGISTRATION:	N° 05-2114511441-65-0000

2. Typical chemical properties

Composition          :  Alkaline earth aluminate

Molecular Formula		 :  MeO·xAl2O3·ySiO2:Eu

(Me=Ca、Mg、Sr、Ba；x=0.5—2.0，y=0.005—0.5)

Insoluble in           :  organic solvents

Decomposition by      :  Acids, water, alkalies

3. Typical physical properties

Appearance            :  yellowish

Specific gravity         :  3.6g/cm3

Temperature resistance   :  250 C°

4. Typical luminescent properties

Excitation              :  UV radiation, white light (any visible light)

Excitation wavelength     :  200-450nm

Peak value              :  520nm

Glowing Color           :  yellow-green

Brightness of afterglow    :  >12 hours

According to DIN67510,Part1

5. Brightness testing report

| Item | CC.Phos Green 2535 |
| --- | --- |
| Time(minute) | Brightness (mcd/m2) |
| 0 | 11220 |
| 1 | 1904 |
| 5 | 563 |
| 10 | 301 |
| 20 | 153 |
| 30 | 103 |
| 40 | 76 |
| 50 | 61 |
| 60 | 51 |
| 85 | 35 |
| Average Particle Size(um) | 25-35 |

NOTE:

Brightness of the pigment of different production batch will be little different, but we guarantee the product accords with our quality standard.